Project Notes

Click here to enter text.

Specimen Notes for 'M8'

Click here to enter text.

| Map Sum Spectrum |  |  |  |  |
| --- | --- | --- | --- | --- |
| Element | Line Type | Weight % | Weight % Sigma | Atomic % |
| O | K series | 8.45 | 0.14 | 13.20 |
| Si | K series | 84.73 | 0.35 | 75.39 |
| Fe | K series | 1.70 | 0.05 | 0.76 |
| C | K series | 5.11 | 0.36 | 10.64 |
| Total |  | 100.00 |  | 100.00 |

| Spectrum 8 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Element | Line Type | Weight % | Weight % Sigma | Atomic % |
| O | K series | 20.40 | 0.64 | 32.31 |
| Si | K series | 70.37 | 0.62 | 63.50 |
| Fe | K series | 9.23 | 0.32 | 4.19 |
| Total |  | 100.00 |  | 100.00 |